## Slide 1: Low Embrittlement Cadmium Plating
6/2020

## Slide 2: Scope
Application of a porous low embrittlement electroplated cadmium coating for corrosion protection of high strength steel
Coating is applicable for electroplating steel parts having a ultimate tensile strength of 180,000 psi or greater

## Slide 3: Classes and Type
Class 1 – 0.0005 inch thick (min.)
Class 2 – 0.0003 inch thick (min.)
Class 3 – 0.0002 inch thick (min.)
Type I – as plated with no supplemental treatment
Type II – with supplemental chromate treatment

## Slide 4: Overview
Requirements
  Training
  Processing Requirements
  Test Specimen Requirements
  Plating Property Requirements
Procedures
  Solution
  Plating
  Treatments
  Stripping
  Repair and Rework

## Slide 5: Applicable Documents
AMS-QQ-P-416
MIL-STD-870
BPS 4006

## Slide 6: Requirements –Training
Annual training
  Review processing requirements
  Test specimen requirements
  Plating property requirements
  Procedures

## Slide 7: Training
Responsibility
  Solution contains cyanide and cadmium
  Wear appropriate safety and health protection equipment
  Comply with
    EPA – 40 CFR Part 413
    OSHA – 29 CFR 1910.1200 Hazard Communication
    North Carolina Permits – 15A NCAC Sections 2Q.0508
  Chemical information is found in Safety Data Sheets (SDS)

## Slide 8: Processing Requirements
All brazing, welding, forming, machining, and heat treating shall be done prior to plating
Parts machined, ground, or formed after heat treat shall be stress relieved
Parts shall be abrasive cleaned before plating
  Excessive metal removal by abrasive cleaning shall be avoided to protect against loss of shot-peen (compressive) layer

## Slide 9: Processing Requirements
Current density shall be maintained at 50 – 70 amps/ft2 for MIL-STD-870
Current density shall be maintained at 20 – 40 amps/ft2 for QQ-P-416 and BPS 4006 (These processes have a 1-minute strike at 60 ASF.
Auxiliary anodes shall be used for holes and recess areas
  Open holes depth > hole diameter
  Blind holes depth > ½ hole diameter
  Recess depth > ½ recess width

## Slide 10: Processing Requirements
Embrittlement Relief of parts within 4 hours after plating
Embrittlement Relief of parts with 4 hours after stripping
Type II Chromate Treatment shall be applied unless Engineering Drawing specified

## Slide 11: Test Specimens
Plating Appearance, thickness and corrosion resistance shall be 4” X 6” X 0.040” SAE 4130 Steel
Plating Adhesion shall be 1” X 4” X 0.040” SAE 4130 Steel
Embrittlement test specimens shall ASTM F 519, Type 1a.1

## Slide 12: Plating Property Requirements
Appearance
  Dull matte gray finish
  Free from blisters, nodules, pits, and other harmful defects
  Shall not exhibit any bright or lustrous areas
    Bright areas are caused by low current densities or by organic contamination and are cause for rejection
  Stains or discoloration resulting from rinsing or embrittlement relieving shall not be cause for rejection
  Type II chromate treatment shall be yellow to brown
  Nickel strike shall be smooth, fine grained, adherent
  Nickel strike shall be free from blisters, pits, nodules, indications of burning, or other harmful defects

## Slide 13: Plating Property Requirements
Plating Adhesion
  Clamped in a vise and bent back and forth until rupture
    Show no separation between basis metal and plating at, or near, the point of rupture when examined at 4X magnification
  Sample is 4” X 1” X 0.040”

## Slide 14: Plating Property Requirements
Plating Thickness
  Thickness is based on class
Class | Minimum Thickness (Inches) | Maximum Thickness (inches)
1 | 0.0005 | 0.0007
2 | 0.0003 | 0.0005
3 | 0.0002 | 0.0003

## Slide 15: Plating Property Requirements
Corrosion Resistance
  Type II, Classes shall show no white corrosion after 96 hours exposure to salt spray
  Test panels shall be aged 24 hours prior to salt spray
  Samples are 4” X 6” X 0.040” panels

## Slide 16: Plating Property Requirements
Embrittlement Relief Testing
  Samples are ASTM F 519 1a.1
  Samples shall be plated to Class 1 or to specification requirements
  Shall pass a sustained load equal to 75% ultimate notch tensile strength for 200 hours.
  Shall show no indication of cracks or failure.
  If one fails, an immediate repeat of embrittlement relief testing is required
  If a second failure, immediate termination of production plating operations and no further plating work shall be conducted until operating problems have been resolved

## Slide 17: Procedure
Solvent Clean to remove oil and grease (WP 316)
Stress Relieve Parts, if required
Mask areas not to be parted (WP 69)
Dry abrasive blast clean (WP 458)
  Aluminum Oxide 120 Grit
  40 to 60 psi
  3 – 12 inches from nozzle to part
  As close to 90 degree between part and nozzle

## Slide 18: Procedure
Rack parts, using auxiliary anodes (WP 495)
Immerse in water to remove abrasive particles
Immerse in hydrochloric acid if strike plating is needed
Immerse in rinse water to remove hydrochloric acid
Immerse in strike plating if needed
Immerse in rinse water to remove strike plating solution
Spray rinse before immersing in cadmium plating tank

## Slide 19: Procedure
Immerse in cadmium plating tank. Apply current at required amperes per square foot. Class 2 plating thickness will be deposited in approximately 11 minutes(WP 474, WP 451, WP 457, WP 450)
Remove parts from plating tank after current is turned off
Rinse with water
Rinse in hot water to help with drying
Unpack and damask
Use clean compressed air to dry

## Slide 20: Procedure
Embrittlement Relief within 4 hours after plating (23 hours minimum baked) (WP 490)
Reactivate surface in water for 15 to 30 seconds
Immerse in Chromate treatment for 15 to 30 seconds
Immerse in water for 30 – 60 seconds
Dry with clean compress air
Allow chromate treatment to cure for 24 hours minimum

## Slide 21: Procedure
Stripping (WP 476)
  Plated parts that require coating removal shall be stripped in ammonium nitrate for 60 minutes.
  Parts require to be embrittlement relief for 23 hours at 375 F within four hours after stripping
  Parts can skip embrittlement relief after stripping if parts are replated within the four hours baking after plating at 375 F

## Slide 22: Procedure
Rework and Repair
  Areas requiring rework because of thickness requirements or minor handling damage may be repaired using LHE cadmium brush plating

## Slide 23: Process Control
Solution Control
  Weekly Tests
Corrosion Test
  Monthly
Thickness
  Lot
Visual Examination
  Lot – Samples and Parts
Adhesion
  Lot
Embrittlement Test
  Monthly

## Slide 24: Pyrometry – AMS 2750
Temperature Sensors (MS #)
Instrumentation (MS #)
Thermal Processing Equipment (MS #)
System Accuracy Test (SAT)
Temperature Uniformity Surveys (TUS)
Label shall include:
  Instrument Number
  Date the calibration was performed
  Due Date of the next calibration
  Identification of the technician who performed the calibration
  Limitations or restrictions of the calibration